出國報告（出國類別：進修）

參加新加坡民航學院機場工程

第二階段訓練班報告書

服務機關：行政院飛航安全委員會

姓名職務：助理工程師／王建發

出國地區：新加坡

出國期間：民國98年7月25日至8月21日

報告日期：民國98年10月22日

目次

1.目的	2

2.行程	2

3.課程安排	3

4.心得	5

4.1航機操作區幾何設計	5

4.2大地工程	14

4.3機場設施電路	18

4.4機場空調及通風系統	19

4.5行李處理系統	20

4.6空橋設計：	21

4.7航機停泊引導系統ADGS（Aircraft Docking Guidance System）	22

4.8機場排水設計	23

4.9瀝青混凝土之理論及實務	26

4.10柔性鋪面設計	33

4.11柔性鋪面施工	36

4.12剛性鋪面設計	38

4.13剛性鋪面施工	41

5.建議	47

1.目的

本次課程是由新加坡民航學院、新加坡南洋理工學院及CPG公司共同開辦，為國際民航組織所承認之訓練，該課程內容結合學術面、實務面及全球規範訂定。此行主要的目的是：（一）了解機場工程之輪廓，（二）培養機場工程施工之種子學員，（三）提昇國內機場安全調查之知識與技巧。

2.行程

行程概述表

| 日期 | 起訖地點 | 行程紀要 | 備註 |
| --- | --- | --- | --- |
| 7/25 | 台北至新加坡 | 啟程 | 中華航空 |
| 7/27-8/21 | 新加坡 | 受訓課程 | 新加坡民航學院 |
| 8/22 | 新加坡至台北 | 回程 | 中華航空 |

學員，包括斐濟、海地、新加坡、韓國、非洲、尼泊爾、中國、泰國

等共18人。新加坡民航學院位於新加坡漳宜機場西北方，方便來自於世界各地的學員參與。

3.課程安排

- 課程簡述：

該課程提供完整之技術性知識，以評估機場發展需求計畫、機場發展設計、機場設施、執行相關工程及維護機場設施等。該階段屬於機場工程之第二階段，所介紹之課程涵蓋航機操作區幾何設計、場址準備、大地工程、土壤穩定、鋪面設計及施工、瀝青混凝土理論及實務、排水系統設計、電力系統、預鑄工法、航廈施工及管理等以達成學員通盤了解機場施工相關學識。

二、授課教師：

本次課程共聘請17位各方專業之講師，其來源背景除機場從業人員外，另自產官學界聘請專業人士擔綱。

課程講師表

| Nanyang Technological University |
| --- |
| Prof Henry Fan | Professor & Director Center for Infrastructure Systems School of Civil and Environmental |
| Assoc Pro Wong Wai Fan | School of Civil and Structural Engineering |
| Assoc Prof Lum Kit Meng | School of Civil and Structural Engineering |
| Assoc Pro Wong Yiik Diew | School of Civil and Structural Engineering |
| Assoc Pro Anthony Goh | School of Civil and Structural Engineering |
| Assoc Pro Chu Jian | School of Civil and Structural Engineering |

| Changi Airport Group (Singapore) Pte Ltd |
| --- |
| Mr Teoh Eng San | Project Manager Project Development & Contract Management Division |
| Ms Koh Sim Yi | Project Manager Project Development & Contract Management Division |
| Mr How Choon Onn | Division Head Project Development & Contract Management Division |
| Mr Stuart Ralls | Project Manager Project Development & Contract Management Division |
| Mr Ong Siong Ka | Executive Engineer (SAS) Engineering & Master Planning Division |

| CPG Consultants Pte Ltd |
| --- |
| Mr Kueh Lip Kuang | Vice President (Airport Civil & Structure) Airport Civil & Structural Engineering Branch |
| Mr Khin Maung Lin | Senior Consultant (Mechanical) Airport Mechanical & Engineering Branch |
| Mr Lee Chong Hee | Vice President (Airport Engineering) Airport Civil & Structural Engineering Branch |
| Mr Lee Ngai Hung | Vice President (AM & E) Airport Mechanical & Engineering Branch |

| BNP Associates, Asia Pte Ltd |
| --- |
| Mr Benedict Onn | Regional Director |

| Skaarup and Jespersen Design |
| --- |
| Mr Poul Mork | Guest Lecturer |

4.心得

## 4.1航機操作區幾何設計

（一）機場分類：

第一要素：aircraft reference field length由製造商提供；

第二要素：Wing Span ,Outer main Gear wheel Span。

（二）跑道幾何設計：

結構鋪面(structural pavement)

道肩(shoulder)

跑道地帶(Runway Strip)

跑道端安全地帶(Runway End Safety Area)

緩衝區(Stopway)

清除區(Clearway)

（三）主跑道長度：

訂定主跑道長度需考量下列因素，包含航機操作性能、航機起降重量、機場高程、機場參考溫度、最高及最低之高程(沿跑道中心線)，另需考量風、溼度、需求最長跑道航機、駕駛員技術、道面狀況及航空公司程序等因素能被計算入內。影響跑道長度需求有安全法規、機場環境、航機起降重量等因素。

美國FAA以航機性能、起降重量、高程及參考溫度發展出圖表錄於FAA A/C150/5325/4A,Runway Length Requirement for Airport Design.決定步驟分為a.決定起飛跑道長度：參考最大起飛重量、機場高程、溫度，每尺高程差增加10尺長標準定出；b. 決定起飛跑道長度：參考航機及引擎型式、最大落地重量、高程，增加濕滑跑道情況7％。選擇起飛或落地較長跑道為其跑道長度。當考量單引擎失效之繼續起飛及放棄起飛，需設置停止區及清除區。

（四）作業詞彙：

1.V1：Decision Speed駕駛員決定繼續起飛或停止之速度，

2.VR：Rotation Speed駕駛員開始拉機頭的速度，

3.Vlof：Lift-off Speed航機已完全離開地面的空速，

4.V2：Take-off Safety Speed航機高於35呎，但單發動機失效，維持爬升梯度，所需之最小速度，

5.起飛距離：Take-off Distance航機高度為35呎，但單發動機失效距跑道頭之距離；航機高度為35呎，但全發動機操作時距跑道頭之115％距離。

6.起飛長：Take-off Run跑道實際長度

單發動機失效時

0.5【Lift-Off Distance】＋0.5【Take-off distance】

全發動機操作時

115％【【Lift-Off Distance】＋0.5【【Distance to 35】－【Lift-Off Distance】】】

7.加速停止距離：Acceleration-Stop Distance

【Accelerate to V1＋Decelerate to Stop】

8.緩衝區：Stopway為航機達V1放棄起飛而超出之實際跑道長度。

【Acceleration-Stop Distance】－【Take-off Run】

9.清除區：Clearway

【Take-off Distance】－【Take-off Run】

（五）安全法規包含降落、起飛、爬升階段之限制：

1.降落：

提供航機通過跑道頭時高50英呎
提供航機停止距離為機場規劃落地距離/0.6 
Landing dist = Distend to stop /0.6 (1)

2.起飛：
（i）單發動機失效
    （a）繼續起飛
         T/O distance = Distance to 35ft height（2）
    （b）放棄起飛
         Field length = “Accelerate-Stop Dist”（3）
 （ii）正常起飛
      T/O distance = 1.15【Distance to 35ft height】（4）
    ＊Field length = Max【(1)(2)(3)(4)】

並非所有的T/O distance 均為Full strength pavement (FSP)

3.清除區(Clear Way, CLW)：為單發動機失效時之一虛擬面
（1）＞150m寬
（2）從end runway upward 1.25% slope
（3）不可有障礙物穿越

4.緩衝區（Stop Way, STW）：為放棄起飛之一實面
（1）＞＝跑道寬
（2）避免航機結構受損
（3）為放棄起飛航機滾行所需

（六）跑道數及跑道方位：需滿足ICAO 95％之利用率。

（七）平行跑道間距：

考量使用VFR或IFR。當平行非儀器跑道可同時使用時，依據ICAO Code number1,2,3,4，最小平行跑道間距應分別為210,150,120公尺；當平行非儀器跑道可同時使用時，依據ICAO Annex14、Doc4444、Doc8168，最小平行跑道間距應分別為1035公尺for independent parallel approach；915公尺for dependent parallel approach；760公尺for independent parallel departure；760公尺for segregated  parallel departure。

（八）航機重量：

航機重＝空重OWE＋乘客貨物重PL＋燃油重Fuel

Fuel＝Trip Fuel＋Reserve Fuel

Takeoff Wt= OWE+PL+Ft+Fr<=最大起飛重量MTOW

Landing Wt= OWE+PL+Fr<=最大降落重量MLW

空重OWE(Operating weight empty)crew and equipment

零油重ZFW crew、equipment and payload

（九）考量機場環境：（Airport Environment）

1.跑道梯度
       最大允許梯度 1-2%

平均均勻梯度(Average uniform grad):

elevation of runway ends/Runway length
       有效跑道梯度:

○elevation of highest and lowest difference/Runway length

2.表面溫度：
           表面溫度增加1℃跑道長度增加0.7~1.3%

3.高度：

高度增加1000ft跑道長度增加7%

4.風：

尾風增加跑道長度增加

5.跑道表面情況：

溼跑道須較長跑道

積水效應為Standing water（hydroplaning）is function of

Vp = 9P0.5

允許水深小於10mm

橫斷溝：5mm寬, 5mm深, 25mm 間距

6.道肩： 須能容忍噴流

7.跑道地帶：需設置

8.跑道端安全地帶：

寬大於2倍跑道寬

為儀器跑道undershooting/over running runway

9.噴流板：

放置於跑道尾端避免起飛噴流傷到鋪面

（十）橫剖面梯度：
1.1%＜橫剖面梯度＜1.5%    為排水功能

2.在跑道地帶前3m梯度可大於5%

（十一）縱剖面梯度變化：

D = n (1x1+1y1+1y1+1z1) or 45m which ever is greater

n = 5000m-Code 1,2

15000m-Code3

30000m-Code4

D = 375m

（十二）視野要求：

CDE code 須於3m高可見至少0.5倍長跑道

（十三）滑行道種類：ICAO Definition

滑行道為提供機場內各部之連結

- Aircraft stand taxilane-機坪內停機位間的連結

- Apron taxiway-機坪間的連結

- Rapid exit taxiway-連結跑道之高速滑行道

（十四）滑行道設計原則：

  - 提供每一跑道一平行滑行道

  - 直接提供滑行道（減少滑行距離＜5km，可以不用繞路走）

  - 提供至跑道頭支流

  - 最少穿越跑道數

  - 提供充裕的彎道空間及彎道加寬設計

  - 提供塔台可見性，避免交通瓶頸

  - 允許提高交通量

（十五）滑行道幾何：

駕駛艙應跟隨滑行道中心線而行，輪淨距為輪外緣距滑行道邊線之距離。ICAO以Code Number II定義滑行道坡度及視距，其最大縱坡度率為每30 m不超過1﹪，意謂所有點的半徑需大於3000m。其坡度取樣為任二點高程差/水平距離。

滑行道道肩shoulder：

有四個主要功能

- 預防發動機超出滑行道邊界，吸入石頭或其他物體，損害發動機，或是造成噴流影響後面飛機。

- 支援航空器發生突發狀況，而不會造成場站實質破壞。

- 支援RFF車輛

- 預防滑行道有異物入侵。

（十六）滑行道地帶Taxiway Strip：

當翼展寬大於滑行道寬時，需定義滑行道地帶。可降低飛機操作時，如滑出滑行道時所造成的損害風險。Visual Aids需低於引擎高度。定義graded area可為非鋪面但可承重而不下沉之結構組成。其中Upward slope of grade area為以相鄰之滑行道坡度為參考線非為水平參考線。

（十七）滑行道安全間距Separation Distance：

Annex 14定義之Taxiway/Runway；Taxiways；Taxiway/Object, Taxilane/Object之間之安全間距。

（十八）滑行道彎道：

ICAO Annex14提供最大滑行速度和滑行道半徑對照表。飛機外主輪與滑行道邊界也不能小於規範值。

（十九）滑行道交界：三種方式解決滑行道交界輪距淨空

- 加寬：將彎道內側加寬，

- 位移：位移其滑行道中心線，

- 兩者結合

雖然(2)及(3)法較為經濟但並不適用夜間低能見度情況

Fillet加寬設計說明見諸ICAO Aerodrome Design Manual-Part 2； AC 150/5300-13

加寬設計模擬可用Software Path Planner為Auto Turn來模擬。

（二十）出口滑行道與快速出口滑行道：

目的在增加最大跑道容量，減少跑道被佔用之時間，ICAO建議當尖峰小時交通量小於25架次時可使用正交出口滑行道。當使用快速出口滑行道時，跑道及平行滑行道間距需大於180m，而25°＜出口滑行道中心線與跑道中心線之夾角（30°佳）＜45°。

（二十一）出口滑行道之位置及數量需考量：

（a）Distance from threshold to touchdown

（b）Touchdown speed （S1）

（c）Initial exit speed（S2）

（d）Distance from touch down to exit taxiway=

（S1）²-（S2）²/2a ,a=deceleration rate

（二十二）等待機坪Holding Bays：

ICAO定義為一個區域能使航機等待，執行有效的旁流移動，在高交通量的機場，提供某預期交通量，為調校導航系統為目的，並考量航機使用量、機型、進入及離開之方式及翼尖淨距wing up clearance。位置需放置於敏感區critical area外避免干擾降落助導航設施。

（二十三）機坪Apron：

機坪指的是提供飛機載、卸人貨郵件、加油、停車、維修之處，aircraft stand指的是飛機停放區域。機坪型式有terminal apron; cargo apron; remote parking apron; service and hanger apron，停機型式有nose-in、nose-out、angled nose-in、angled nose-out、parallel，機坪設計需考慮翼尖淨距，航機尾流等。

（二十四）服務區設備：

可能有hydrant fuelling point；ground rods；electric power outlet；preconditioned air supply；pneumatic air supply；potable water supply；Pax boarding bridges.

（二十五）航機轉彎半徑計算：

## 4.2大地工程

- 土壤材質：

- Coarse-grained巨粒土、粗粒土（sand砂, gravel碎石, cobbles卵石, boulders礫石）

碎石、卵石：具有較高強度及穩定性，可用來填築土基（subgrade），但由於石隙較大，其上之結構層易脫空，所以機場道面一般不採用。

礫石：由於粒徑較大，內摩擦係數亦大，因而強度和穩定度均能滿足要求。

砂土：透水性強且無塑性，毛細上升高度很小，具有較大的內摩擦係數。但由於黏性小易鬆散、壓實困難，可用震動法或有條件之情況下，添加黏性大的土以提高穩定性。

砂性土：粒徑介於砂土與粉性土之間，含有一定數量粗顆粒，使土基具有足夠強度和水穩定性；又含有一定數量細顆粒，使其具有黏結性，不致過份鬆散，是修築土基理想材料。

- Fine-grained（silt粉性土 ,clay黏性土 , colloid重黏土）

粉性土：含較多粉土顆粒，浸水後易形成稀泥。毛細作用強烈，水分上升快速。在冰凍地區，水分積聚嚴重會引起土基凍脹，春融期間易形成翻漿。必須用粉性土修築土基時需傪配其他材料，改善其性質。

黏性土：細顆粒比重大，內摩擦角小，黏結性大，透水性小，吸水能力強。吸水時膨脹，乾燥時收縮，毛細現象較顯著，乾燥時較堅硬，不易被水浸濕，但潮溼後難以乾燥使強度大大降低，須充分壓實並採取很好排水措施。

- 級配：各國訂定不同區分之分類土壤，較佳等級（well grade soil）土壤，

其gradation curve較平彎向上，反之較差等級（pool well grade soil）土壤，

其gradation curve較陡峭。

- 加州承載比CBR：CBR是美國加利福尼亞州公路局提出一種評定基層材料承載能力的試驗方法。承載能力以材料抵抗局部荷載壓入變形的能力表徵，並採用標準碎石的承載能力為標準，以相對值的百分數表示CBR值。由於CBR的試驗方法簡單，設備造價低廉，在許多國家得到廣泛應用。採用CBR法確定柔性道面厚度，有配套的圖表，應用十分方便。

- 土壤滲透性Permeability of Soil：

V = discharge velocity = K*I = permeability coefficient *hydraulic gradient = K*h/l  Hydraulic head distance

同一地區，在自然條件相同下，土基的強度在很大程度上與其相對含水量有關。土基含水量較小時，強度較高。反之，則較低。土的穩定性下降，也常常是由水的侵害造成的。

- 土壤特性：相位圖及其計算

- 土基填築：

Land Reclamation two ways:dumping & hydraulic fill(傾填、液態填充)

Land Clear：Vegetative Growth；Job specification； Soil Condition or Bearing Capacity；Topography；Rainfall & Climate

填方施工前土基作業區及借土區的草皮上、種植土、腐植土、樹叢、樹根、淤泥等應清除乾淨。土基基底原狀土的土質不符合設計要求時，應進行換填，換填深度應不小於30公分，並應按要求的密實度予以分層夯實，方允許在其上填築。土基填築應分層填築、分層夯實。當石塊級配較差、粒徑較大、填層較厚、石塊間空隙較大時，可在每層表面的空隙裡填入石屑、石渣或中、粗砂等細料，再用震動壓路機反覆碾壓，使空隙密實。

土基填土宜採同類土，至少要求各層填土用同類土，同時應將透水性強的土壤填在上層。當土基填土石混合料時，若岩性和土石混合比相差太大時，應分層或分段填築。如不能分層或分段填築，應將含硬質石塊的混合料鋪於填築層下面，同時石塊不能過分集中，上層再鋪含軟質石料的混合料，然後整平碾壓。

土方開挖時，對計畫用在土面區的植物土和其他表土應存放在指定地點，不同類的土不應混雜堆放。土方開挖應自上而下進行，不得亂挖、超挖，如遇特殊土質時，應報請監理工程師和設計部門提出處理方案。

土面區內的溝、坑、塘等不要求進行特殊處理，但應排除積水，晾乾淤泥。土面區填方地段的植物土可不挖除，但應清除樹根、草叢和稻根。

- 夯實Compaction：充分夯實的土基可以發揮土基的承載強度，減少土基和道面在機輪荷載作用下產生的形變。夯實可使土壤有較低可壓縮性、增加剪力強度、減少滲透性、增加土壤之長期強度，故夯實過後之土壤可降低分子間距、降低空氣體積。考慮經濟因素下，使用Mechanical , Chemical, Thermal, Electrical穩定法穩定土質，其中Mechanical Stabilization及densification為夯實。

三種夯實試驗：

(1)Standard Compaction(Proctor)test

(2)Modified AASHTO Compaction test

(3)Vibrating Hammer test。

低含水量之土壤很難夯實，當含水量加大，水佔據空氣空間易求得最大乾密度，但當含水量太多時減低乾密度反而不易夯實。

Degree of compaction = dry density = (d = Ms/Vt = (bulk / 1+W

在頂點意謂可藉增加或減少土中含水量

使逹到最大夯實度及最大乾密度 (最佳)

- 夯實的方式：

根據土質狀況合理選擇夯實機械，對提高土基的壓實效果有十分重要的作用。採用光面壓路機(roller 、sheet-foot roller)碾壓時，由於碾輪與土基接觸面大，單位壓力較小，因此光面壓路機的夯實厚度較小。施工中，通常用輕型或中型光面壓路機進行預壓，適宜用於低黏性土、黏性土，不適用於無黏性的砂。

輪胎壓路機(pneumatic-tired rollers)是利用充氣輪胎及其懸掛裝置的可變性，使輪胎與土基表面保持一定的接觸面。由於他可以調節本身總重量，與被壓土層接觸面積大及有效夯實深度大，因而日益廣泛地被用在各種大地工程的夯實操作中，適合黏性土。

震動壓路機(Vibratory)夯實功能很高，機上的調節裝置可以根據需要調成不震、弱震或強震的工作狀態。適合低黏性土、砂礫料及碎石混合料。用震動壓路機壓實非黏性土時，而土的含水量為最佳含水量的1.10~1.20倍時，能得到較好的夯實效果，但需注意將震出的水及時排出。

- 壓密及壓密沉陷(Consolidation＆Consolidation Settlement)：

土基夯實的好壞對道面使用性能和壽命影響較大，一旦土基夯實不佳給道面帶來危害，則很難處理。大型飛機有效作用深度可達4~5米，因此對土基頂面以下1~4米範圍內填方的密實度都有較高要求。民用機場道面往往在土基施工後很快即開始鋪築，土基沒有足夠的自然沉降時間。因此除了控制密實度外，還應對土基總體沉降量及不均勻沉降量加以限制。

發生壓密的原因在於土壤顆粒變形，內含之水及空氣，因而被擠壓出來。當氣孔內水被擠壓出來，土粒重新安排其結構，變得更穩定及緊密，體積因此減小，土表沉陷，該過程發生的快慢決定土壤滲透性，該土壤重組程度決定於土壤骨材剛性，如黏土加壓致水分由氣孔擠出的過程為應力應變及時間關係。

## 4.3機場設施電路

（一）CCR（Constant Current Regulators）function功能：

- Produce a constant current output

- 2 and more output current when dimming of the light are required.

Key considerations of HT network:

- Ensure at any one time a single cable fault will not affect the entire network system 任一個單一電纜故障不會影響全部系統

- A single transformer failure will not affect the outgoing circuits

- Adequate interlink between intake sub stations are available

- Protection coordination 協力防護機制

- Ring load should not exceed 80% of cable capacity

- Critical load centres provide with multiple feeds

- Limit the number of substations to 4 to 5 per ring

（二）機場使用串聯電迴路：

- 可用較長線路 Longer cable length

- 一串定亮度 uniform lighting intensity for entire CCR

- 高壓For Primary CCR 5KV(no. of lights

- Secondary CCR(isolating 防止burn

（三） Power supply to mechanical equipment

1. For large mechanical equipment, they are powered from dedicated sources 有專用電源

And circuit breaker shall be adequately sized to cater for high starting current 迴路斷路器能承受高初始電流

2. For smaller, they are powered from sub-board in respective floor or from mains LT switchboard when the loading is larger 從本身層板供電

3. To keep transformer load at about 60%~70% capacity for future expansion and power surge 維持變壓器在60%~70%承載以應變突然的大電壓

## 4.4機場空調及通風系統

1.目的：

Useful and widely used: CO2 sensor to modulate the amount of fresh air to save energy

Proper air filter: high efficiency, UV, charcoal

相對溼度高於65% 易滋生細菌、黴菌。

2.負載估計 Load Estimation：

Heat sources:

- Solar radiation

- Heat conduction, wall, partition

- Heat interior human, facilitate generation

- Fresh air(ventilation流通空氣), Infiltration

3.中央空調系統Central air condition System

4.通風井功用  Mechanical Ventilation：提供新鮮空氣、控制味道及濃煙及防火功能。

## 4.5行李處理系統

- Out bound Baggage Handling System (OBHS)

- 三種BHS：

Automated System； Semi-Automatic System ；Manual System

（2）Sortation System

- Manual Sortation
 economic, easy maintains, reliable

- Automated Sortation System
 (i)    Tilt-tray System(用傾斜tray托盤將baggage導出
 (ii)   Pusher system(用推出器將baggage導出

(iii)  Destination Code Vehicle Sortation system高速昂貴

（3）Output / Make-up Device：Sortation後裝箱的出口
(i)  Make-up loop：need more space, few flight together, equal access
(ii)  Lateral loop：1 lateral 1 flight, walk baggage to container
(iii)  Slides： more, manpower, 分等裝箱

2.Automatic System Design Consideration

(1) Bar Code tag；Radio Frequency ID 
(2) Failure Mode

(3) Cost effective

3.Security Equipment

- Detecting explosive

- False alarm rates

- Through put

- Person training

4.Inbound Baggage Handling System
(i) flat plate device－simple low cost, friendly

(ii)Inclined Plate device－fast, effective, complex & space, injury

## 4.6空橋設計：

- 乘客空橋設備：

- Rotuna: 包含一個固定部位支持tunnel and the fixed gangway，另一個可移動部位和tunnel相連可上下左右動。

- Tunnel: 可分成2~3個部份，第1個部分和rotuna相連，其他部分合在一起可以伸縮

- Wheel carriage(under carriage): 左右各可以轉動90度

- CAB: 可縱向旋轉65度

- 4種PLB型態：

- Pedestal Type－90(懸臂；

- Apron Drive Type－可多向調整，Aircraft也可多方式停放；

- Radial Drive Type－不可前後移動，因為無套筒可swiveling，但可旋轉；

- Over the wing Type－可跨越機翼

- Advantages of using PLBs

- 在惡劣天氣情況下，舒適及便利保護乘客上機

- 改善大飛機載貨處理效率

- 減少車輛危害及擁擠情形

- 降低延誤率及障礙

- Disadvantage od using PLBs

- 建置費及維修成本

- 空橋基本設計考量： 
(1) 航機停止位置
   (i) Proximity to building or finger pier
   (ii) Tail limit
   (iii) separation between adjacent gates
   (iv) fuel hydrant outlets
(2) 空橋斜度

slopes of the bridge when docked to the aircraft <10%, adjusting the height of rotunda and shifting the stopping position of the aircraft

(3) 可操作之範圍Operational Range of the Bridge
sufficient operational range to serve all the types of the aircraft

空橋安全考量：Safety Consideration
(1) Fail Safe Design : Fail then turn to safety Mode

設定錯誤會回復到正常狀態

(2) Auto leveler : 機門防撞，載卸貨時自動微調高度

(3) Limit Switches : 預防和他橋碰撞 2 Sets of limit switches, protect other apron users and equipment

(4) Fire Protection : NFPA 415

## 4.7航機停泊引導系統ADGS（Aircraft Docking Guidance System）

調整航機走向利用雷射光數測量航機azimuth, closing rate, stopping guidance 於顯示板中提供予駕駛員參考，包含對準停機坪中心線及停止位置，提供到離資訊予飛航資訊顯示系統。可提高機坪效率、降低勞工、降低機坪間距等優點。

## 4.8機場排水設計

機場排水系統旨在阻止場外水流入場內，促使場內水迅速排至場外，可分為四個主要組成部分。

- 調節部分：直接吸收土中多餘水分或直接攔截表面水的排水構築物，如道面邊緣和土質地區的蓋板溝等。

- 導水部分：將各調節部分所匯集的水導至容泄區的管路。

- 容泄區：用於容納或排走機場多餘水分的區域，如機場附近的河流、湖泊、地下透水層等均可作為容泄區。

- 排水系統中的其他構築物：如防止機場水淹的防洪堤，明、暗導水線路相接處的出水口，為便於檢查、維修暗導水線路而設的檢查井等。

機場排水工程的質量和進度直接影響到飛行場內其他工程的施工，尤其是道面混凝土的施工。安排排水施工時，應依據｢先場外、後場內｣、｢先下游、後上游｣、｢分段施工、分段完成｣等原則安排好與其他工程的施工順序，避免互相干擾。

｢先場外、後場內｣是要先做好場外的排水工程，可以避免暴雨或洪水淹沒機場，保證場內排水工程施工的正常進行，然後再做場內的排水工程。

｢先下游、後上游｣是只排水溝的的施工應按先下游後上游的施工順序，使得在施工過程中雨後即可排除積水，不會影響施工的進行。

｢分段施工、分段完成｣是指不宜全面開花，因為一般排水線路都比較長，應該完成一段後再轉入下一段，以免欲速不達而影響工程質量與進度。

要設計排水溝的高度寬度必須先了解該機場的洪水量，能使排水溝足以負荷。以及坡度的設計，以避免流水所產生的震動過大影響道面的壽命。計算公式參考如下：

- Estimate of Surface Runoff

- Coefficient of Run off, C
                       ( 查表

- weighted runoff coefficient

- Time of Concentration Tc
    Time of surface flow overland flow inlet time Ts

Time of flow within the drainage system Td

Tc = Ts + Td  (Distance, C 查表)

- Rainfall Intensity I
    5 年洪水量 + 下雨時數 ( 查表

- Run off rate ( Rational Method
    Q = run off =     = C*I*A/360 （mm/hr）（hectares ha）
    1ha = 10,000 m2

- Hydraulic Design of Drain

- Manning Formula

Discharge capacity: Q

flow area: A

drain material roughness coefficient: n

- V = Q / A = average velocity

- Froude Number   need<1
    Fr = V / gy1/2     Fr<1  sub critical condition

- Design Consideration

- 1 < V < 3  m/sec steady flow
1.5m/sec for earth stream

- subcritical Condition    Fr < 1
         avoid unstable & wary in critical condition

- Freeboard : 15%

- Transition : 15W

- Bend In drain : R > 3W

- Drainage Sump : > 1.5W

- Open Drains in critical Area not allowed

## 4.9瀝青混凝土之理論及實務

一、瀝青種類Type of Asphalt
    Hot mix : Asphalt cement熱拌瀝青混合料，在瀝青混合料中最典型的品種，採用高稠度的石油瀝青為結合料，經過高溫加熱和強制拌和，凡是不冠以特加說明的瀝青混合料，就是指這類混合料。
    Cold mix : Cutback asphalt ; asphalt emulsion乳化瀝青是瀝青(石油瀝青、煤瀝青等)經機械作用分裂為細微的液滴，分散在含有表面活性物質(乳化劑、穩定劑)的水介質中，由於乳化劑吸附在瀝青微滴表面的定向排列作用而降低水與瀝青界面間的界面張力，使瀝青微滴均勻的分散在水中，不致產生沉析。同時，由於穩定劑的作用，使瀝青微滴在水中形成均勻穩定的分散系。具有高流動度，可以冷態使用，並能與潮濕礦料有良好的黏附性。因此使用乳化瀝青修築路面具有節約能源、保護環境、便利施工、降低造價等優越性。

二、瀝青膠泥組成Component of Asphalt Cement
    asphaltenes, resins, oil 瀝青混合料是一種複合材料，它是由瀝青、粗集料、細集料和礦粉以及外加劑所組成。

三、瀝青混凝土分級系統AC Asphalt Grading system

針入度分類(CNS 2260)

40~50、60~70、85~100、120~150、200~300

黏度分類(ASTM D3381或AASHTO M226)

AC 2.5、AC 5、AC 10、AC 20、AC 40

AR1000、AR2000、AR4000、AR8000、AR16000

hard                 soft

  - Penetration針入度     25℃   40, 50, …            200,300

  - Viscosity 黏度         60℃   AC40, AC10,…       AC2.5

  - Viscosity aging        60℃   AR16000, …         AR3000

  - Performance    PG 58-28 ( -28℃ < perform < 58℃

四、Cutback Asphalt 油溶瀝青: hazard from fire & toxicity

又稱塗料柏油為柏油與石油溶劑混合製成之液體產品，容易流動，使用時可免加熱。使用塗料柏油之後，當中所含的溶劑逐漸揮發，會留下強韌的柏油膜。可因其所含溶劑揮發快慢的不同，塗料柏油又分為特快乾、快乾、及慢乾料柏油三小類

for curing : reduce viscosity by plus solvent
    Rapid curing (RC)(AC + gasoline) ;

Medium curing (MC)(AC + Kerosene);
    Slow curing (SC)(AC + low volatile oils)

Workability, curing time, viscosity after curing

五、Emulsified Asphalt乳化瀝青 :

asphalt particle in water with emulsion agent
    cationic : asphalt particle (+) (good for – aggregate)
    anionic : asphalt particle (-)
    係以瀝青加溫磨成小顆粒狀，加入乳化劑與水強力混和，使瀝青小顆粒懸浮於水中，待水分蒸發後會還原成瀝青。乳化瀝青依凝結速度區分特快凝（RS）、快凝（MS）及慢凝（SS）三種，依所帶電荷之不同，分陽離子及陰離子兩種。

六、Aging 產生是因為高溫使Asphalt cement內含的Oil揮發氧化或因暴露於外界環境中。

七、瀝青品質測試：

瀝青（asphalt）提供包裹粘結粒料、防止水分滲入等作用，我國所用瀝青材料幾乎全為提煉石油副產品。瀝青依其軟硬程度分成數級，以往採用針入度分類，目前逐漸改用粘度分類。

瀝青針入度試驗係以25℃瀝青樣品，量測用標準試驗針以100g總質量貫入5秒鐘之深度（0.1mm）（圖11），針入度越大表示瀝青越軟。針入度試驗容易，但比較不容易反應瀝青之工程性質，目前已 逐漸少用。國家標準目前公佈有二種瀝青標準，分別為CNS 2260 [鋪路柏油（瀝青）－針入度分級]及CNS 15073[鋪路柏油（瀝青）－黏度分級]。

瀝青粘度試驗以往係採用玻璃粘度試驗管，測取瀝青流經固定距離所需時間，再按試管之校正係數換算成粘度。粘度越大表示瀝青越硬，亦即針入度越小。玻璃粘度試驗管作業困難，目前逐漸採用旋轉式粘度計，將瀝青樣品放入金屬試管中以60℃定溫，置入一枚不鏽鋼轉子在其中按指定速度旋轉，測其扭力，利用電腦溫控及試驗，作業方便。粘度分類又分AC及AR兩種方式，AC分級以原始瀝青之粘度為準，AR分級以滾動薄膜熱損試驗（RTFOT）後之瀝青粘度為準，試驗過程較繁，我國除特殊情況外，路面工程大多採用AC分級。

瀝青可依針入度或粘度分許多等級，應視氣溫條件選用合適等級之瀝青。我國以往常採用85/100針入度或AC-10，目前高速公路及中低海拔省道已改用AC-20。在60℃時，AC-10之粘度為1000 poises，AC-20則為2000 poises。有部分特殊工程採用改質瀝青（瀝青材料中添加橡膠、聚合物等，改善瀝青之感溫性及提高強度）。

八、粒料：提供pavement主要load bearing的能力

粒料約佔瀝青混凝土質量之95％，擔任提供主要體積、承載荷重、抵抗變形、產生抗滑表面等作用。粒料之材質、粒形、級配會影響其性能。我國常用密級配及開放級配兩種，前者空隙率小可防水份滲入，後者空隙率大可讓水分快速排除。

（1）粗粒料

A.粗粒料（停留於2.36mm（8號）篩上者）應為優良之石材等軋製之碎石，須潔淨、質地堅硬、緻密、耐磨及級配良好者。

B.以重量計，粒料中至少應有75%為碎石顆粒，且扁平狹長之顆粒（寬度與厚度之比或長度與寬度之比大於3者）不得超過10%。

C.粗粒料依洛杉磯磨損試驗（CNS 490）500轉後之磨損率，用於磨耗層者不得大於35%，用於面層者不得大於40%，用於底層、聯結層及整平層者不得大於50%

D.粗粒料經5次循環之硫酸鈉健度試驗（CNS 1167[使用硫酸鈉或硫酸鎂之粒料健度試驗法]），其重量損失不得大於12%。

E.粗粒料應依尺度大小分別堆放，並應避免互相混雜，俾能正確按規定比例混合，其混合程序應在冷料供應系統上完成。

（2）細粒料

A.細粒料（通過2.36mm（8號）篩者）包括石屑、天然砂或兩者之混合物。

B.細粒料經5次循環之硫酸鈉健度試驗（CNS 1167），其重量損失不得大於15%

C.如需用二種以上不同來源之細粒料時，應分別堆放，其混合程序應在冷料供應系統上完成。

九、瀝青混凝土的要求考量：

瀝青混凝土應由合格瀝青拌和廠產製，我國普遍採用分盤式拌和廠

- 穩定性（Stability）：有足夠之強度，以承受交通荷重，扺抗塑性變形之能力，不致於使路面發生扭曲變形現象。

- 柔性（Flexibility）：係指路面受荷重時，底層雖發生變形或撓度，但不龜裂，而能恢復之性質。

- 耐久性（Durability）：瀝青混合物中有足夠之瀝青含量及足夠之粒料強度，以扺抗交通荷重及氣候影響之下所產生之粒料鬆散及剝脫等現象。

- 抗疲勞性（Fatigue Resistance）：可承受重複輪重所引起之彎曲作用而不龜裂。

- 抗滑性（Skid Resistance）：抵抗車輪剎車滑動之能力。

- 工作性（Workability）：瀝青拌合料具相當流動性，使易於鋪築和滾壓，而不致於發生粒料分離現象，以及能達到應有之壓實度。

- 密緻性（Impermeability）：防止空氣與水份滲入之能力。

十、製造瀝青混凝土：Manufacture Asphalt Concrete

在相同原料情形下，瀝青混凝土之性能主要受其粒料級配及瀝青含量影響，粒料級配及瀝青含量有多種設計，表5所示為ASTM D3515 （熱拌瀝青路面混合料規範）所建議之部分密級配瀝青混凝土要求。表6所示為美國加州之底層用粗級配瀝青混凝土要求。

## 4.10柔性鋪面設計

  - 航機路徑機率

    - Aircraft Path deviation from Center Line
Landing Runway > Take off runway > Taxiway

    - Maximum Repetition of Load (Max damage)
Greatest damage occurs for channelzed condition(Taxiway)
Taxiway ( Center of main Gear
Runway ( Center line of Runway 因為 ( deviation (

    - 二種計算法wander effect
(i) Portland Cement Association (PCA) Method
  。Load Repetition Factor
(ii) FAA Method
  。Convert traffic to coverage
  。Coverage : number of Max stress application occurring  within the pavement due to applied traffic
  。One coverage : Each point in traffic lane pavement has
    experienced a maximum stress
  。Pass-To-Coverage Ratio(表可查
    =  No. of Departure / Coverage 
     小飛機 coverage 小；大飛機 coverage 大

    - Highly Channelized traffic on Taxiway, Runway End, Turn off area

  - Soil分類

FAA Method 先分Partical Gradation (Size),再分Plasticity constant

三、Equivalency Factor

- 目的在於將Stabilized course 轉成Granular course

- Layer thickness, stabilizing agent type, quality, and location of stabilized Layer.

- Minimize Bituminous Surface ≧10cm critical；≧3in no critical

四、Overrun area pavement

≧1/2 runway pavement thickness；more stone chip aggregate

五、Aircraft Load

- 95﹪ weight on Main Gear

- Landing gear type & Geometry(Single, dual, dual tandem, wide body)

- Tire pressure ：75—200psi

六、Development of Flexible Pavement design curve

- CBR method

- Develop for single wheel loading (convert all type to single wheel)

- Adjust by load repetition factor (base on annual departure over 20 years)

- Designed A/C: greatest thickness (Type & annual departure)

七、Design Equivalent Annual Departure for design aircraft

- Convert different type A/C：

1.Annual departure to designed A/C；

2.Make wheel load（MTOW*0.95）/N

- Each Type annual departure by designed A/C make by Log R1 ＝√W2/√W1

- Summation Each type to be Equivalent Annual Departure for design A/C

- Wide body designed to be 136100；dual Tandem

八、求出Flexible Pavement Design Thickness

查表並使用Equivalent Annual Departure for design A/C；MTOW；CBR for subbase & subgrad求得Total pavement thickness ；考慮另一表，minimum base course thickness equipment

九、Overlay 原則

- 不可使用sandwich 因為separation granular layer不利排水

- Overlay最少瀝青厚度為75mm

- 可將Surfacing視為Base course

- Base course視為Subbase course	equivalency Factor

十、ACN-PCN Method

ACN(Aircraft classification Number)：

A Number expressing the relative effect of an aircraft on a pavement for a specified standard subgrad strength

PCN(Pavement Classification Number)：

A number expressing the bearing strength of a pavement for unrestricted operations.

PCN bearing strength /pavement type(R,F) /sub grade category(A,B,C,D,E) / Tire pressure(W,X,Y,Z)/ evaluation(T,U)

## 4.11柔性鋪面施工

- 各層特性：

- Subgrade：Compact to dry density 95%；Stabilized with cement

- Transition Layer：To prevent migration of fines into sub-base

- Sub-Base：Intermediate layer used to add thickness to the pavement and also to distribute wheel loads over a greater area. Better quality on top of sub-base layers (well graded granular；more permeable than the base permit drainage & no-plastic material) Plasticity Index < 6

- Base：Material need tough；PI<6% 小 plastic；Dense gradation with n=0.4 to 0.6 where Pd=(d/D)^n x100%；High strength

- Wearing Course：High stability；High skid resistance；Open-graded mix 20%；Air void for wet weather and prove good skid res.

- 比較Batch Plants & Drum Mix Plants

Batch Plants: 30% of U.S. asphalt production

缺點: spilling of other sizes of a aggregates into hot bins

會溢滿到熱儲箱

Drum Mix Plants: 70% of U.S. asphalt production

優點: 使用較低溫於drum mixer內，less oxidation, 較快速混合

- 鋪築機：Asphalt Paver

  - Tractor unit：

Provides power to drive the paver

組成：truck push roller；hopper；Auger；conveyor

控制：Material feed system control by conveyor speed；screw speed；flow gate opening；control amount of material

(二)Screen Unit：

To establish the thickness of the asphalt concrete layer

AOA control by low point & thickness control cranks

AOA (angle of attack)     material thickness

(三)Automatic Screen Control：

Propose: To ensure constant amount of mix delivered to the screed by automatically adjusting the:

Speed of slat conveyor

Flow gate opening

Speed of the augers

Principle: elevation of two point is kept constant and permits a constant angle of attack even if the tractor unit moves up and down vertically

上高地時    Pull point      AOA constant

下坡時		 Pull point      AOA constant

- 瀝青混凝土滾壓：Asphalt concrete Rolling (compaction)

(一)三種滾壓機

(1)Steel wheel：Three-wheel steel Roller；Tandem Roller275—415 KN/m2

(2)Pneumatic Tire Static Roller：275-862 KN/m2

(3)Vibrating steel wheel roller：Frequency vibration

(二)控制夯實之變數：Control compacting variables

      - Magnitude of load：Static weight, dynamic force, Total force

      - Frequency of Vibration：2000-2400 Vpm

      - Roller speed: effects on density, 2.5 mph

      - Number of Roller Passes: density  , uniformly

      - Rolling Zone>125℃

      - Roller path: uniform

(三)柔性鋪面之夯實：

- Sub grade and embankment fill by all type of roller for granular aggregate cohesive soil by pneumatic tired

- Base & Subbase：Heavy vibrating drum or steel wheel roller for granular

- Asphalt Surface：3 stay of rolling；Thin mat not to use vibratory roller

(1)breakdown rolling: T>125℃using steel wheel roller

(2)Intermediate rolling : T>80℃using pneumatic or vibrating roller

(3)finish rolling : T>65℃using steel tandem roller

## 4.12剛性鋪面設計

- 剛性鋪面組成：Component：PCC Slab；Subbase；Subgrade

Sub base: No need if no frost hazard；Its functions are for mud pumping, frost action, deformation, supporting

Subgrade：Need to be compacted

- 影響剛性鋪面設計因素：

  - Aircraft traffic Volume depend Aircraft departure traffic；

  - Aircraft load；

(3)Strength of Subgrade-Subbase or both

(i) subgrade –compact造成dry density上升；降低lower moisture content；提高強度。

K=modulus of subgrade reaction=rate of increase in the compressive strength of subgrade=<500 pci (136 MN/m3)FAA recommend

(ii) subbase：well grade crushed aggregate

Standard thick= 4 in but now check for > 45400 kg load impermeable

- 混凝土橈度強度：Concrete Flexible Strength

FAA規範flexural test 於7,14,28,90天取樣測試

Module of rupture(flexural strength , psi)= Elastic Module 8-10 constant√Compressive strength of concrete , psi (MR =K √fc)

- 剛性鋪面應力：Wheel load; temperature 、moisture differential friction及Stress due to friction

(1)Wheel load：from FAA interior loading；Edge loading

(2)Temperature & moisture differential：Temperature differential造成Curling及Warping Stress；Moisture 造成的bend 方向和Temperature相反可互相抵銷。

  - Stress due to friction

Slab & Subgrade produce due to temperature differential

- 美國航空總署剛性鋪面設計方法：FAA Method of Rigid Pavement Design

Westergrad’s analysis of edge loaded slab of jointed edge rigid pavement

先求出Aircraft Annual Departure Volume, N

再將Concrete Flexural Strength, Subgrade Module, Aircraft Gross weight W；查FAA表；rigid pavement thickness required

- Pavement Joints 功能及分類：

- 功能：允許熱脹冷縮不至於分離；釋放因Temperature & moisture content產生slab 及foundation間的摩擦力；Construction 所需。

- 分類：Construction Joints；Expansion Joints；Construction Joints

- Construction Joints：

        - Longitudinal Construction Joints：At edge of each construction lane；Keyed & download to provide load transfer；Tie bar hold slabs together

        - Transverse Construction Joins：butt type Joint with dowel使用在暫時停工，在預劃縮縫位置附近；keyed joint with tie bar使用在預劃位置間隔Middle Third處。

- Expansion Joints：Provide space for expansion；Not used in rigid airport pavement；二不同材料相接時才需要Expansion Joints；pavements thickness < 10 in 時及 placed during cold weather 時需要

- Contraction Joints：Predetermined location；Relieve tensile stress；Controlling cracking；Sawed or formed groove type。

- Joints Chart：

|  | Expansion Joints | Construction Longitudinal | Construction Transverse | Contraction Longitudinal | Contraction Transverse |
| --- | --- | --- | --- | --- | --- |
| Key | X | V | V | X | X |
| Dowel | V | v | V | X | V |
| Tie bar | x | v | V | v | X |

- Joints Spacing：當without stabilized subbase時width B/t(in) <24, length L <1.25 B；當stabilized subbase,所以higher warping and curling stress；4—6=Joints space/radius of relative stiffness

- Jointing Steel：

- Tie bar：用在 longitudinal contraction joints & construction joints；不可承受力量只負責接合

- Dowels：允許transfer load across joint；prevent relative vertical displacement of adjacent slab end

- Reinforced Rigid Pavement：可解決角型易破碎帶的問題

Log R=log R 2 √w2/w1

## 4.13剛性鋪面施工

- Two construction method:

a) Manual Method

For minor pavement works within restrained areas where machine paving is not feasible

少部分受限制於機器無法加鋪的情形下，即用手工方式。

b) Mechanized Method 有2種施工法：

a. Fixed form Paving固定式：Used for construction at smaller aircraft pavement area or area where slip-form machine is not able to perform the work. 使用於小型飛機鋪面場或滑動式機械無法施工時

b. Slip-form Paving滑動式：Used for construction of airfield pavement>200mm thick. 使用於場站鋪面厚度大於200mm時，能夠使較深層混凝土更堅固。

Advantage：機械化優點

- Quality control：better and consistent quality 品質較好且一致

- Production speed：higher production rate 較高生產率

- Labours：less labour dependent 節省人力

  - 施工材料：

(1)~(4) Concrete

  - Aggregate: coarse and fine mix

Not more 8% for elongate flat size < 5cm

  - Cement:

Ordinary Portland Cement (OPC)

Rapid Harden Portland Cement (RHPC)

Portland Blast Furnace Cement (PBFC)

Asphalt Resisting Portland Cement

Portland cement:

    - Most widely used

    - Able to provide moderate resistance to sulphate and moderate heat of hydration (抗sulphate侵蝕及熱氣)

    - High early strength

    - Low heat of hydration

    - High sulphate resistance

  - Water: Clean

  - Admixture: 7 type chemical admixture

Type A: Water-reducing

Type B: Retarding

Type C: Accelerating

Type D: Water-reducing + retarding

Type E: Water-reducing + accelerating

Type F: High range water-reducing

Type G: High range water-reducing + retarding

Accelerating Admixture:

- Accelerate setting and early strength gain in concrete

- Usually used in cold weather and urgent repairs of pavement where reduction in setting is critical 通常用於冷天氣及緊急修補鋪面時

Retarding admixture:

- Delay initial and final setting times in concrete

- Usually used in hot weather concrete and at situation where long haul time of concrete delivery is inevitable 在熱天氣需長時間搬運的混凝土，降低其固化速率

Water-reducing admixture:

- Reduce water/cement ratio (w/c) at given workability

- Increase workability for a given water content

降低(水/水泥)比例，需要使用時再增加水

Function：

- Produce a system of air bubbles in the cement paste to allow freezable water to expand so that it does not damage the internal structure of concrete 在水泥漿產生氣泡體，用冰水使它展開不會破壞內部結構

- Improve workability of concrete

- Reduce bleeding, segregation and water demand in fresh concrete

- Overdose air-entrainment admixture reduces the concrete strength; 1% increase in dosage give 5% reduction in concrete compressive strength. 夾帶過量氣體會降低混凝土強度

注意其Workability；Reduce bleeding segregation；Improve frost resistance

  - Curing Covering material表面養護材料

White Burlap + polyethylene sheet包覆防止水分流失

Water-proof paper/white polyethylene sheet

Liquid Membrane Forming Compound形成包膜

Function：

- Maintain relative humidity in concrete surface above 80% for 7days

可維持混凝土表面之相對濕度80%達7天

- Form a tough, firm surface to withstand construction traffic

堅固的表面足以應付預期交通量

- Pigmented curing compound recommended as they make it easy to verity proper application.(The white pigment in curing compound helps to reflect sun’s heat) 人工的養護化合物之其他用途

  - Joint Filler

Preformed expansion joint filler(non-extruding and resilient

bituminous type) 預期膨脹之縫隙裝填(非擠壓及有彈性的瀝青材)

Preformed sponge rubber and cork expansion joint

海綿橡膠或軟木裝填

Backer Material for cold and hot applied sealants in Portland

Cement Concrete and Asphalt Joints

  - Joint Sealed / Sealant

    - 2-component jet blast resistant, cold applied joint sealants

    - Hot-poured, elastometric joint sealant for Portland cement concrete pavement

    - Cold applied, single component, chemically curing silicone joint sealant for Portland cement concrete pavement

  - Joint Insert

Not a basic product for pavement works. Can be either proprietary or improvised product. 非基本配備可自行斟酌使用

  - Steel Reinforcement

    - Welded steel wire fabric (welded fabric) reinforcement

    - Welded deformed steel wire fabric

    - Reinforcing Bar Mats

  - Tie Bar and dowel Bar

如講義圖

- 混凝土混合限制：

(1) Minimum Flexural strength of Concrete

600psi(4.15 MPa) at 28 days

(2) Minimum cement content

564  (227 )

(3) Maximum allowable water/cement Ratio (w/c)

w/c<0.45

(4) Workability of fresh concrete (slump):

用一模型將混凝土倒入夯實，然後lift out模型，測量混凝土下降

高度H

Low slump rate (1-2 cm) good to slip

Fixed-form 1”~2”

Slip-form 0.5”~1.5”

(5) Cementations Material：

Fly ash substitution: 20%~30%

Ground blast furnace slag: 25%~55%

crash < 25% ; Ground slag < 30%

(6) Air entrainment in concrete mix

% of air entrainment depends on max. aggregate size and

concrete exposure level, 2%~7%

- 裝備：Equipment

(1) Batching Plant: Bins and Hopper; Scales

(2) Mixer: Central plant Mixer; Truck Mixer and Truck Agitator;        Non-agitator Truck

(3) Placing and Finishing Equipment:

Finishing Machine: Oscillating-type transverse; Screeds; Vibration;

side-form: surface pan type; internal type; Hand vibration

slip-form: Internal vibration; Vibrating screed

Paver: Placing, consolidating, finishing the concrete pavement

- 開始準備 subgrade and subbase preparation:

accurately trimmed; proper elevation and profile; subgrade and subbase need moister with water without saturate; for slip-form, widen SB and SG, to support paver. 夯實及測試密度，調整修正梯度與適當高度，Land strip 兩側至少比加鋪車多1m寬，視需要對下層重複夯實及測試

- 處理測量計算及群組材料:

Aggregate: different stockpiled: drainage, dry; secure, no mix

measured within 2% accuracy by weight

Cement: measured within 1% accuracy by weight

Water: measured within 1% accuracy by weight

Admixture: measured within 3% accuracy

- 混合混凝土：

Mixing Time: 50-90 second; Mix to place: 30 minute non-agitating; 90 minute-agitating;

Mix limitation: heat aggregate or water in cold water;	>10℃ place cold aggregate or water in hot water; < 35℃ in place.

- 放置混凝土Placing concrete：

No placing under insufficient natural light

Placing and spreading;

Strike-off and placing reinforcement.

- 放置Joints

Longitudinal joints-construction

Transverse joints-contraction, construction

- 完成Consolidation and Finishing；

- 紋理Texturing；

a. Brush or broom finish

b. Burlap drag finish

c. Artificial turf finish

above for taxiway etc.

d. Skid-resistant surface: for runway

Saw-cut groove

Plastic groove

Wire combing

- 養護Curing

Entire completed pavement cured for > 7 days

In cold weather concreting, entire concrete cured > 50℉ (10℃)

a. Impervious membrane method

b. Polyethylene film or water-proof paper

c. White burlap polyethylene sheet

- Quality Control of Works

Acceptance sampling and testing:

a. Flexural strength

b. Pavement thickness

Other acceptance criteria

- Slip form Paving 的優缺點：

優點：不需加框可節省材料、人力及建置時間； usually equipped with

multi-function accessories, placing, spreading, consolidating,

finishing 所需不同機械在同一步驟可完成，較有經濟效益。

缺點：newly後置強化要形成混凝土鋪面較為困難；newly stand-alone

pavement lane易受天氣破壞，天氣變壞時需增加保護以防雨水侵蝕。

5.建議

新加坡民航學院不僅在專業師資之提供、課程安排，具有完整規劃，對於學員學習成效利用多種形式之考試，了解其吸收能力，相對於其他訓練機構實謂嚴謹，所有學員勢必獲益良多，本次課程僅完成機場施工部份，該課程之第一階段尚有機場系統與規劃、第三階段尚有機場設施及機場工程維護部份尚未完成，本次課程機場施工主要著重於機場鋪面之大地工程與設計，職認為如能將第一及第三階段課程完成，對於機場工程訓練方能完整。

# Text boxes

X%＝ 0.01 y%＝-0.005  z%＝ 0.005